## Slide 1: Test Results of the First Short Coil for the LHC Inner Triplet Upgrade & Short Quadrupole Assembly Test
G. Ambrosio (FNAL)
on behalf of the MQXF team:
M. Anerella, G. Apollinari, R. Bossert, R. Carcagno, D. Cheng, G. Chlachidze,
D. Dietderich, H. Felice, P. Ferracin, A. Ghosh, R. Hafalia, E. Holik, S. Izquierdo Bermudez, M. Juchno, S. Krave, F. Lewis, M. Marchevsky, V. Marinozzi, F. Nobrega, I. Novitski, D. Orris, H. Pan, J. C. Perez, I. Pong, S. Prestemon, L. Rossi, G.L. Sabbi,
C. Santini, J. Schmalzle, M. Sorbi, S. Stoynev, C. Sylvester, M. Tartaglia,
E. Todesco, G. Velev, P. Wanderer, M. Yu, A.V. Zlobin

## Slide 2: MQXF: LHC HiLumi Upgrade
 | Unit | Value
Aperture | mm | 150
Nominal gradient | T/m | 132.6
Operating temperature | K | 1.9
Operating current | kA | 16.5
Peak field at op. current | T | 11.4
Stored energy/length | MJ/m | 1.17
Peak field including strand self field
US-LARP & CERN
LHC Inner Triplet Hi-Lumi Upgrade
P. Ferracin, et al. “Development of MQXF, the Nb3Sn Low-β Quadrupole for the HiLumi LHC” this session
Courtesy of S. Izquierdo Bermudez
Courtesy of P. Ferracin

## Slide 3: Nb3Sn Coils
1st generation short coils (LARP/CERN):
  Practice-test coils: 2/2
  OST RRP coils: 4/3
  Bruker-EAS PIT coils: -/2 in progress
1st generation long coils (LARP):
  Practice: 1 in progress
  OST RRP coils: 2 in progress
2nd generation short coils:
  Starting both at LARP & CERN
E. Holik, et al. “Fabrication and Analysis of 150 mm Aperture Nb3Sn MQXF Coils”, this session
S. Izquierdo Bermudez, et al. “Second Generation Coil Design of the Nb3Sn low b quads for HL-LHC”, 2POBA02
Courtesy of F. Nobrega
Courtesy of J. C. Perez

## Slide 4: LARP coil QXFS2 from practice to test coil
Strain gauge system:
1 azim. + 1 longit. full bridge on inner titanium pole,
4 quarter bridges bonded to inside surface of inner coil,
  used during construction only.
Strand diameter, mm |  | 0.85
Strand composition |  | (Nb -7.5 w% Ta)3Sn
Strand type |  | OST-RRP 108/127
Cable width, mm |  | 18.09
Cable mid. thickness, mm |  | 1.53
Keystone angle, degree |  | 0.52
Twistpitch, mm |  | 109
Number of strands |  | 40
Core (25 um x 11.8 mm) |  | 316 SS
*N. Cheggour, et al., “Influence of Ta and Ti doping on the irreversible strain limit of ternary Nb3Sn superconducting wires made with restacked-rod process”, Supercond. Sci. and Tech., 20, (2010).
Safe strain at RT
< 0.2%
based on strain cycling*
Small bubbles on lead end surface after impregnation
Courtesy of R. Bossert

## Slide 5: Single Coil Test Facility a.k.a “Mirror”
MQXFS Mirror Design is derived from previous Mirrors built at Fermilab by the HFM group
TQ mirror
HFM Dipole Mirror
HQ mirror
MQXFS Mirror
Short mirrors (<2m): bolted
Long mirrors (>2m): welded
A.V. Zlobin, et al. “Testing of a Single 11T Nb3Sn Dipole Coil using a Magnetic Mirror Structure”,
IPAC’2014, Dresden, June 2014
SSL @ 1.9K:
68%
96%
97%
98%
SSL @ 1.9/2.2K:
77%
89%
94%
98%
Courtesy of A. Zlobin, I. Novitski, R. Bossert

## Slide 6: MQXFSM1 SSL
Mirror structure as coil test facility for QC:
  Load line within a few percent from MQXF load line
  Low prestress to avoid damage
T [K] | Bpeak_SS [T] | Icable_SS [A]
4.5 | 13.20 | 18734
1.9 | 14.49 | 21065
Courtesy of A. Ghosh, D. Dietderich, S. Izquierdo Bermudez

## Slide 7: Pre-stress Target
At quench current the azimuthal Lorentz force is ~30% lower than in the quadrupole model
=> lower coil prestress needed:
~80 MPa at 300K
< 140 MPa at 4.2K
< 150 MPa at 12T
Courtesy of I. Novitski and S. Krave

## Slide 8: Actual Pre-Stress and Strain
Press to 80 Mpa azimuthal stress in press without skin or clamps.
Actual – 79 MPa azimuthal
480 µS longitudinal
(increased at every loading)
Drive in side clamps, increasing azimuthal preload to 90 Mpa
Actual – 89 MPa azimuthal
530 µS longitudinal
Install skin, return to press, press to azimuthal preload of 90 MPa.
Actual – 89 MPa azimuthal
310 µS longitudinal
Bolt skin and release press. Final average azimuthal coil preload of 70 MPa.
Actual – 77 MPa azimuthal
270 µS longitudinal
Courtesy of R. Bossert

## Slide 9: Quench Training (1.9K)
All quenches in pole turns (mostly in Inner Layer, a few in Outer Layer)
Limiting point: Inner Layer, Pole turn, Lead End (highest field region)
16.5 kA
78.3% SSL
17.8 kA
84.5% SSL
19.2 kA, 91.3% SSL
Courtesy of S. Stoynev

## Slide 10: Ramp Rate & Temperature Dependence
Quench ramp rate dependence at 1.9 K:
Quench location as in training quenches
No quench in ramp down from
16.5 kA at 300 A/s
Temperature dependence study at 20 A/s
90% of SSL both at 1.9 K and 4.5 K
Holding current test:
No quench:
for 2 hours at 16.5 kA at 4.5 K
for 2 hours at 17.8 kA at 1.9 K
Courtesy of S. Stoynev

## Slide 11: QP Studies and RRR
Inner Layer heaters copper plated
Outer Layer heaters with heating stations
Both heaters performed as expected (delay < 15 ms at 16.5 kA)
130 < RRR < 160 for all segments
Courtesy of S. Stoynev

## Slide 12: MQXFSM1 Observations
Overall this coil performed well and 91% SSL is a good result for a new coil design
  Promising for the 1st short model test
Nonetheless there is some degradation
Possible explanations:
  Excessive strain during assembly for (Nb -7.5 w% Ta)3Sn RRP strand
  Impregnation bubbles may have increased local strain
    Coil is presently spare for 1st MQXFS test
    Will be cut when no more needed

## Slide 13: MQXFS Assembly Overview
Al shell
Iron yoke
Alignment pin location
Iron pad
Iron masters
Load key
Bladder location
Assembly alignment slots
LHe SS vessel
Cooling hole
Titanium pole
Coil
Welding strip slot
Alignment key location
Al bolted collar
Practicing assembly & loading with the first Nb3Sn coils
  Five assemblies to get the final size of the collar shims & alignment key shims.
  Possible damage to some coils during a disassembly phase
  Lessons learned applied to subsequent and future assemblies/disassemblies
Courtesy of D. Cheng, H. Pan and H. Felice

## Slide 14: Assembly iterations
No. | Radial Shim | Pole Key Shim | Pressure Sensitive Film
1 | 1.575 mm | 0 | Yes
2 | 1.524 mm | 0 | No
3 | 1.448 mm | 0 | Yes
4 | 1.448 mm | 0.43mm per side | No
5 | 1.448 mm | 0.46 mm per side | No
MQXFS magnet assembly iterations
Collar pack assembly
Coil subassembly insertion
Bladders are in position
Courtesy of D. Cheng, H. Pan and H. Felice

## Slide 15: Preloading
Chart: Shell Azimuthal Strain (με)
1500psi
2000psi
3500psi
Bladder pressure by quadrant
From 2500 psi to Max: 4200 psi
Load key shims:
50 mil
60 mil
63 mil
Target: 1147 μm
Top
Right
Bottom
Left
Chart: Rod Axial Strain (μm)
1000psi
1500psi
2500psi
4000psi
Target: 819 μm
Azimuthal loading
Axial loading
Preload based on experience from the HQ series
Double SG system LARP/ CERN for comparison during excitation
  => goal is to decide the most efficient system for the long prototype

## Slide 16: Conclusions
The single coil test showed that MQXFS coil design & fabrication technology are fine (up to 90% SSL)
The Assembly Test showed that we can reach target pre-load
We expect Cold Assembly Test to confirm pre-load at 1.9 K
 plan for 1st model test (Feb 2016)

## Slide 17: Extra Slides

## Slide 18: Context of the incident
Normal setup
During the incident
  The center coil support spud was not in place;
  The technicians were removing the side collar pack, the steel angle block was released
Steel Angle block
Coil support spud
Assembly Table
Assembly Table
Return End
Return End
1- Disassemble the top collar stack
2 -Disassemble the collar stack #2

## Slide 19
Incident sequence
Return end view
Coil 104 fell onto the assembly table,
Coil 3 fell into coil 5
Red circles indicate the edge of the coil impacting other coil or assembly table.
03
104
103
05
03
104
103
05
03
104
103
05
Return end view
Ready to disassemble
Collars removed
Coils fell off
03
104
103
05
103
104
104

## Slide 20: Corrective action already implemented
Modification of the spud
To capture the 4 coils
Modification of the procedure to account for missing disassembly steps
Cause analysis process started at LBNL
Will possibly lead to additional corrective actions
See Patricia Thomas’slides

## Slide 21: Short Coil QC (MQXFSM)
Mirror structure as coil test facility for QC:
  Load line within a few percent from MQXF load line
  Low prestress to avoid damage
Bolt on skin
Coil Protective Shell
Coil Midplane shim
Yoke (EDM’d blocks)
Aluminum Side Clamp
Design by
A. Zlobin & I. Novitski

## Slide 22: Quench Locations
No quenches in low field area, only
few quenches in the OL pole-turn
segments
Established plateau quench
pattern:
Simultaneous start in a3_a4 and
a4_a5 segments, QA signals originate
in segments #1 and #2
Data analysis in progress
VT A08
VT A04
VT A03